| ITEM | Specification | Requirement |
| --- | --- | --- |
| Abstract | Outer Size (L) | 471mm |
|  | Outer Size (W) | 371mm |
| Effect Area | F115 Mask Version | Refer to Mask List |
|  | Glass Type | Corning EXG |
|  | Glass Thickness | 500um |
|  | Glass Surface Flatness | ≤0.1um over 20mm |
|  | Glass Surface Roughness | ± 25um over 20mm |
|  | Buffer Layer Thicknesses | SiNx/ SiOx: 500A/ 1300A |
|  | Poly Layer Thickness | 445A |
|  | Poly(N+) | P_12KeV_1.5E14cm-2 |
|  | Poly(P+) | B_20KeV_4E14cm-2 |
|  | ILD Layer Thickness | SiNx/ SiOx: 700A/ 450A |
| Process Requirement | Poly CD (refer to PCR) | monitor only |
|  | N+ CD (refer to PCR) | monitor only |
|  | P+ CD (refer to PCR) | monitor only |
|  | Poly/N+/ P+ Process PEP shift inspection | monitor only |